Bentonite

Technical Specifications:

OCMA Grade

Moisture         : 8-12% weight

Residue (Wet) :2% max.

Viscometer Reading (at 600 rpm):	30-40 cP

Filtrate Volume : 11-16 cm3

Yield Point	 : 18-25 cP

Packaging:  The product  is packed as 40 kg kraft and plastic lined bags, or in 1.000 Kg  big bags.