Where no range is stated, treat data as typical rather than absolute

Drilling Starch / Non fermenting

Storage	store dry, 12 months

Packing	25kg or 50lbs net paper bags with PE coating.

special packing like jungle boxes; optional

Safety Precautions	None. Refer to Safety Datasheet.

Application	Fluid Loss reducer for all types

of drilling fluids

Typical laboratory and field data are available for evaluation.

Rate of addition	10 - 30 kg/m3	(4 – 11 ppb)

Properties

Bulk density	650 - 700gr/l

Others	resistant to high concentrations of salt

(sodium, potassium) and calcium compounds.

Stability	suitably preserved with environmental

friendly biocide, stable against bacteria

Particle size	< 2000 micron

Description	low viscous fluid loss reducer

Modification and base	modified potato starch

Appearance	free flowing, granular white powder

Compatibility	all drilling fluids

Solubility/Dispersibility	readily without lump forming

excellent suspensibility

Data Sheet	Drilling Starch exceeding

OCMA DFCP 5 specs and

API 13A, Section 11 (May 1,1993)