LIGHT SODA ASH

Description:

White, powder, hygroscopic, easily dissolved in water, clear and colorless in water solution material. Main compound is Sodium Carbonate.
Standart No: TS 525 TYPE 3B

Chemical Specifications:. Sodium Carbonate, (Na2CO3) (%); 99,10 min.. Sodium Chloride, (NaCl) (%); 0,25 max.. Iron, (Fe) (ppm); 15 max.. Insoluble matter in water (%); 0,01 max.. Sulfate, SO42- (%); 0,027 max.. Physical Specifications:. Structure of the Material; Free flowing powder. Standard density; 0,47 - 0,59 gr/cm3.

Packaging:

In block-bottom laminated polypropylene (PP) bags of 25 or 50 kgs. each.

Palletized and shrink-wrapped 1000 kg. each, containing 25 kg. laminated block-bottom PP bags.

In polypropylene big-bags with polyethylene (PE) in-liner and four loops, 650 or 1000 kgs. each.

In bulk